Granulime® 30

High Calcium Quicklime - Calcium oxide CaO

Granulime is a white granular calcium oxide product which is made by crushing and screening quicklime.

Typical		Specification

Chemical Analysis     (Dry Basis)				% Mass		% Mass

Calcium oxide			CaO			94			90.0 min

Silica				SiO2			1.9

Magnesium oxide		MgO			0.42

Aluminium oxide		Al2O3			0.23

Ferric oxide			Fe2O3			0.13

Carbon			CO2			2.7			6.0 max

Sulphur			SO3			0.04

Physical Analysis

Reactivity 			Time (Mins)		Temp. C

0			20

2			25

5			33

10			48

15			54

20			56

Particle Size*			Millimetres		Passing %		Passing Range %

40			100			100

28			96

10			23

5			4

Bulk Densities			kg/m3			700

Specification Based on in Process testing of Burnt Lime 40 Feedstock.

*Specification Based on in testing of Granulime 30.

This specification relates to product numbers: 	130001 - BULK		Last Revision Date: May 2018	131001 - IBC1000/IBC1100

133501 - IBC500

133001 - IBC350

132001 - IBC300

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime®  60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.